## Slide 1: Late stage ideas from early development
How structural informatics approaches can transform pharmaceutical processes
Andy Maloney
Particle Science Team Leader
18th November 2022

## Slide 2: Structural Informatics
A
B
Which is the stable wall?
The database of walls
indicates that A is the
frequently observed arrangement and therefore the one that achieves stability.
My House
c.1967
Great Wall
of China
c.1368
Great Pyramid
of Giza
c.2560 BC
Hadrian’s Wall
c.122
The CCDC
c.1992

## Slide 3: The Cambridge Structural Database (CSD)
Chart: Year
| < 1973 | 1974 | 1975 | 1976 | 1977 | 1978 | 1979 | 1980 | 1981 | 1982 | 1983 | 1984 | 1985 | 1986 | 1987 | 1988 | 1989 | 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Total structures | 13176 | 15169 | 17311 | 19485 | 22221 | 25314 | 28733 | 32611 | 36865 | 41531 | 46765 | 52016 | 58527 | 65444 | 72317 | 79792 | 87442 | 95195 | 104144 | 114091 | 124797 | 136857 | 149135 | 162132 | 177682 | 193583 | 210832 | 229429 | 249091 | 270487 | 294372 | 320177 | 347667 | 378826 | 413055 | 448989 | 485402 | 525973 | 567584 | 611825 | 659233 | 707354 | 758215 | 811947 | 868286 | 925810 | 980876 | 1037884 | 1098658 | 1152585
New | 1993 | 2142 | 2174 | 2736 | 3093 | 3419 | 3878 | 4254 | 4666 | 5234 | 5251 | 6511 | 6917 | 6873 | 7475 | 7650 | 7753 | 8949 | 9947 | 10706 | 12060 | 12278 | 12997 | 15550 | 15901 | 17249 | 18597 | 19662 | 21396 | 23885 | 25805 | 27490 | 31159 | 34229 | 35934 | 36413 | 40571 | 41611 | 44241 | 47408 | 48121 | 50861 | 53732 | 56339 | 57524 | 55066 | 57008 | 60774 | 53927 | 27459
CSD Refcode ELOFUJ
The 1.1 millionth CSD structure
A CSD Communication determined by Bill Clegg
>1,206,500
Structures published that year
Structures published previously
The CSD. Acta Cryst. (2016). B72, 171-179
> 1.1 million structures
  >94M 3D coordinates
> 28 million bond lengths
  >2M unique distributions
> 40 million valence angles
  >3M unique distributions
> 14 million torsion angles
  >800K unique distributions
> 2 million rings
  >400K unique distributions

## Slide 4: Characteristics that influence stability
Molecular
Conformation
Hydrogen Bond
Donor/Acceptor Pairing
Hydrogen Bond
Geometry, Symmetry
and Motif
‘Non-Hydrogen Bond’
Intermolecular
Interactions

## Slide 5: CSD derived knowledge bases
Mogul: I. J. Bruno et al., J. Chem. Inf. Comput. Sci. (2004), 44, 2133-2144
IsoStar: I. J. Bruno et al., J. Comput.-Aided Mol. Des. (1997), 11, 525-537
Mogul
Number
of hits
Tosion angle (º)
Molecular geometry distributions
Bond lengths
Valence angles
Torsion angles
Rings
IsoStar
Intermolecular geometry analysis
Interaction distributions displayed as scatterplots or contour surfaces
18,000 pre defined interaction scatter plots

## Slide 6: Intramolecular geometries
N. A. Tamayo et al., J. Med. Chem. (2015), 58, 4462–4482
Computational method: SCRF-B3LYP/6-31G* dihedral scans
Mogul provides histograms in < 10 seconds per torsion angle

## Slide 7: Intermolecular interactions
central group: -CONH2
contact group: NH
Search for structures containing desired contact
Superimpose hits and display as scatterplots or contour plots

## Slide 8: Combining plots into Full Interaction Maps
P. A. Wood et al., CrystEngComm (2013), 15, 65–72
Molecule is broken down into fragments
IsoStar maps for each fragment are combined to give the Full Interaction Map
Multiple maps can be generated for different probes

## Slide 9: Where do our workflows fit?
Molecule
Form
Particle
Properties
Solid Form Informatics
Particle Informatics

## Slide 10: CSD-Materials
Hydrate Analyser &
Solvate Analyser
Crystal Packing
Similarity
Motif Search &
Packing Feature Search
Conformer
Generator
Full Interaction Maps
Hydrogen Bond
Propensity
Molecular
Complementarity
Solid Form Assessment
Solid Form Investigation
Solid Form Prediction
Aromatics Analyser

## Slide 11: The “Health Check” methodology
N. Feeder et al., J. Pharm. Pharmacol. (2015), 67(6), 857-868

## Slide 12: CSD-Particle
Identification and analysis of potential slip planes
Visualisation and analysis of surface properties
Morphology calculations
M. J. Bryant et al., CrystEngComm (2018), 20, 2698-2704
M. J. Bryant et al., Cryst. Growth Des. (2019), 19, 9, 5258-5266

## Slide 13: Particle Informatics
Descriptors | 
Physical | Chemical
Reticular Surface Area | Functional group analysis
Rugosity | Hydrogen bond donor/acceptor density
RMSD, skewness, and kurtosis | 
Peak Analysis | Aromatic bond density
Statistically derived interaction data | 

## Slide 14: Particle Informatics
Facet
Physical descriptors
Chemical descriptors
Facet
Physical descriptors
Chemical descriptors
Aggregated particle properties
Wettability
Sticking
Compaction
Flow

## Slide 15: Ibuprofen punch sticking
Ibuprofen forms different morphologies depending on crystallisation solvent
Same facets, different ratios and surface areas
H. Cano et al., J. Cryst. Growth (2001), 224, 3-4, 335-341
Ethanol
Ethyl Acetate
Higher Sticking Propensity
Lower Sticking Propensity

## Slide 16: Particle properties
Higher Sticking Propensity
Lower Sticking Propensity
A.A. Moldovan and A.G.P. Maloney, in preparation

## Slide 17: The digital future?
Crystal Structure Predictor
Sticky?
Forms needles?
Tablets well?

## Slide 18: Morphology landscape
Consider small:medium vs. medium:large ratios of a bounding box
Morphology calculations

## Slide 19: Morphology landscape
M. K. Corpinot, L. Iuzzolino, S. L. Price and D.-K. Bučar, unpublished work.

## Slide 20: Morphology landscape
M. K. Corpinot, L. Iuzzolino, S. L. Price and D.-K. Bučar, unpublished work.
S. Kumar et al., Pharmazie (2008), 63, 136 - 143

## Slide 21: How early could we go?
Particle Property Landscape
S:M Ratio
M:L Ratio
Stickiness
Could we understand process behaviour from a molecular diagram?
How well can we control our landscape?

## Slide 22: Acknowledgements
Solid Form Science and Particle Science teams at CCDC
Members of Crystal Form Consortium, ADDoPT and D-DAP
AMSCI, Innovate UK, Knowledge Transfer Partnerships